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TTII CRYSTAL BRIGHT SPECIFICATION
PHYSIAT
Produced and Distributed from Lake Wales, FL

SUPPLIER:	Target Technologies International Inc 
GRADATION:	16-30 & 30-50 (20-40 special order)
SAND PHYSICAL PROPERTIES:

Shape: sub round to sub angular
Color:	white 
Mohs Hardness:  7
Specific Gravity:  2.65
Si02: 99.59

COATING PHYSICAL PROPERTIES:

Non microplastic acrylic coating 
UV resistant
Stain resistant
Water resistant
Antimicrobial APEO Free, formaldehyde 
                 free, low VOC
Colors:	Full Green and Frosted Green

	TESTING: 

· EPA 1633 PFAS Testing
· ASTM F3188 Toxicology
· EN-71-3 Toxicology
· EPA6020B CAM 17 Toxicology
· PAH’s Toxicology
· Lisport

TYPICAL SIEVE ANALYSIS:
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Sieve Size % Retained
16-30 20-40 30-50

8 0.1

12 0.7

16 7.0 0.2

18 13.6 1.3 0.1
20 246 7.9 0.8
25 29.1 214 1.9
30 11.1 23.9 26.1
35 7.0 23.6 40.0
40 3.7 14.1 20.5
45 8.1
50 23 7.1 1.9
60 0.4
70 0.1
Pan 0.0 0.5 0.0





